## Slide 1: The Impact of the “Lazy S” Defect on the Mechanical Properties of a Self-Reacting Friction Stir Weld on Al 2024-T4
Procedures
Conclusions
Future Work
Objectives
Results
Research Undergraduate: Joshua Walters
Advisor: Dr. Michael West
Impact
Acknowledgements:
Thanks to the National Science Foundation grant # 0852057
Drs. Michael West, Alfred Boysen, and Bharat Jasthi, and to the SDSM&T AMP Center.
Test the mechanical properties of a self-reacting friction stir weld that has signs of the “Lazy S” defect
  Objective 1 – Experimentally establish weld parameters that are favorable for the formation of the “Lazy S” defect
  Objective 2 – Test the mechanical properties of the welds to determine if the “Lazy S” defect has any impact on them
Objective 1 Procedures
  Make a series of bead-on-plate style welds using varying weld parameters (Spindle Speed, Travel Speed)
  Analyze the macro-structure of each weld to determine whether the weld is defective
Objective 2 Procedures
  Perform a series of butt joint welds using the parameters established in objective 1
  Test the welds to determine whether the mechanical properties are affected by the “Lazy S” defect
Self-reacting tools are still relatively new in the world of friction stir welding, and are still not entirely accepted as an effective means of joining materials. The research in this project is a step toward making self-reacting tools more acceptable in an industrial setting. The use of self-reacting tools could make many obstacles, such as welding intricate or closed shapes, much more reasonable. This could potentially establish FSW in many significant industries, such as the pipe-fitting or petroleum industries.
Figure 1 Picture of a self-reacting FSW tool
There are many unknown factors that could be further explored regarding the “Lazy S” defect. Its formation in other types of alloys is a major area that could be investigated, as wells as investigating preventative measures to minimize the chance of its formation.
Chart: Vickers Micro-Hardness
| -0.32500000000000051 | -0.30000000000000032 | -0.27500000000000002 | -0.25 | -0.22500000000000017 | -0.2 | -0.17500000000000004 | -0.15000000000000022 | -0.125 | -0.1 | -7.5000000000000094E-2 | -5.0000000000000065E-2 | -2.5000000000000033E-2 | 0 | 2.5000000000000033E-2 | 5.0000000000000065E-2 | 7.5000000000000094E-2 | 0.1 | 0.125 | 0.15000000000000022 | 0.17500000000000004 | 0.2 | 0.22500000000000017 | 0.25 | 0.27500000000000002 | 0.30000000000000032 | 0.32500000000000051
SRT 009 | 132 | 115.55 | 121.65 | 121.9 | 121.3 | 131.85 | 131.2 | 142.7 | 141.15 | 138.9 | 135.6 | 135.35 | 138.75 | 139.55 | 137.65 | 132.75 | 134.55 | 140.25 | 141.3 | 132 | 133.15 | 137.2 | 135.25 | 136.5 | 132.95 | 134.75 | 119.65
SRT 010 | 128.15 | 120.4 | 119.3 | 109.7 | 125.25 | 130.6 | 132.45 | 133.4 | 134.75 | 127.1 | 134.9 | 127.4 | 130.3 | 125.15 | 129.1 | 131.1 | 133.55 | 125.5 | 127.1 | 128.15 | 124.9 | 130.35 | 125.65 | 135 | 129.25 | 120.7 | 116.65
SRT 011 | 136.35 | 115.25 | 119.1 | 125.3 | 133.15 | 134.9 | 137.2 | 135 | 140.7 | 141.7 | 135.25 | 135.25 | 132 | 132 | 142.35 | 140.95 | 143.75 | 130.85 | 138.65 | 136.35 | 134.25 | 134.15 | 142.75 | 138.95 | 135.65 | 119.3 | 118.1
SRT 012 | 141.95 | 119.75 | 129.2 | 127.25 | 138.85 | 140.95 | 141.3 | 148.5 | 151.05 | 141.15 | 140.95 | 146.3 | 143.2 | 139.75 | 142.2 | 141.45 | 140.55 | 139.2 | 142.15 | 141.95 | 144.3 | 132.8 | 139.75 | 139.55 | 136.85 | 131.05 | 121.65
2024-T4 Al | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1 | 145.1
Figure 3: The “Lazy S” defect near the root of a weld
Figure 2: Clamping mechanism for the self-reacting tool
Based on the discoveries of the experimentation, the “Lazy S” defect has a significant impact on the mechanical properties of a self-reacting weld made with 2024-T4 Aluminum. The research found that while micro-hardness measurements showed minute differences in hardness, the tensile properties of the welds were substantially compromised by the presence of the “Lazy S” defect. The defect contributed to the initiation of cracks during tensile testing, and, in the case of welds 011 and 012, made up the entire fracture surface.
Metallographic analysis revealed an observable “Lazy S” formation in all the butt welds performed in the experiment. After mechanical testing was performed, it was discovered that while the micro-hardness was relatively unaffected, the tensile properties of the welds were severely compromised. Welds that had greater signs of the “Lazy S” formation had a considerably lower peak stress during tensile testing.
Sample | Average Peak Stress (Ksi) | Peak Stress (% of Base Metal) | Average Elongation (%)
Base Metal | 71.2 | n/a | 20.2
009 | 47.4 | 66.6 | 4.4
010 | 49.6 | 69.7 | 3.7
011 | 31.5 | 44.2 | 2.0
012 | 26.0 | 36.5 | 0.2
Figure 4
Top: Highlighted “Lazy S” defect
Bottom: Tensile Sample Crack
Figure 5: Tensile Samples before testing
Table 1 Tensile Test Data